AQUA GOLD

Aqua Gold Prime

- 50% renewable content

- Enhanced colour generation on timber species

- Extended open time but fast dry time

- Excellent sanding performance.

- Low VOC formulation

TYPICAL PROPERTIES

Appearance;			Milky white, translucent

Solids					25%

Density				0.95

Viscosity				55 cPs (25°C)

pH					6.5

Volatile Organic Content Wt %	10%

APPLICATION PROPERTIES

Recoat time				60 mins @25°C

Dry Time:

Coverage:				10m² per litre

Gloss Level 60° Specular		na

Wash up:				Water