**AQUA GOLD**

****

Aqua Gold Prime

* 50% renewable content
* Enhanced colour generation on timber species
* Extended open time but fast dry time
* Excellent sanding performance.
* Low VOC formulation

**TYPICAL PROPERTIES**

Appearance; Milky white, translucent

Solids 25%

Density 0.95

Viscosity 55 cPs (25°C)

pH 6.5

Volatile Organic Content Wt % 10%

**APPLICATION PROPERTIES**

Recoat time 60 mins @25°C

Dry Time:

Coverage: 10m² per litre

Gloss Level 60° Specular na

Wash up: Water