AQUA GOLD

Aqua Gold “RAW”  ultramatt

- Single component self & 2 k systems available

- Excellent scratch,  wear and chemical resistances

- Excellent levelling and brush drag properties

- Low VOC formulation

- Attar Certified non slip finish, P3 and P5 variants avialable

- Ultramatt finish, resembleing uncoated timber

TYPICAL PROPERTIES				1K				2K

Appearance							Milky white, translucent

Solids						30%  single pack			40%, 2K

Density					0.96					0.97

Viscosity					110cPs @ 25°C			150cPs @ 25°C

Volatile Organic Content Wt %		12%					15%

APPLICATION PROPERTIES

Recoat time					6 hrs @ 25°C			6 hrs @ 25°C

Coverage					10²m/L				10²m/L

Gloss Level 60° Specular			Dead Matt ….			Dead Matt ….

Wash up					Water					Water

Full Cure					5-7 days				5-7 days