**AQUA GOLD**

****

Aqua Gold “**RAW**” ultramatt

* Single component self & 2 k systems available
* Excellent scratch, wear and chemical resistances
* Excellent levelling and brush drag properties
* Low VOC formulation
* Attar Certified non slip finish, P3 and P5 variants avialable
* Ultramatt finish, resembleing uncoated timber

**TYPICAL PROPERTIES 1K 2K**

Appearance Milky white, translucent

Solids 30% single pack 40%, 2K

Density 0.96 0.97

Viscosity 110cPs @ 25°C 150cPs @ 25°C

Volatile Organic Content Wt % 12% 15%

**APPLICATION PROPERTIES**

Recoat time 6 hrs @ 25°C 6 hrs @ 25°C

Coverage 10²m/L 10²m/L

Gloss Level 60° Specular Dead Matt …. Dead Matt ….

Wash up Water Water

Full Cure 5-7 days 5-7 days